# FINISHES
FILM & PENETRATING

## Materials and Techniques

# WHY FINISH?

## Stabilize

### Minimize Humidity Absorption

#### Hygroscopic Wood

## Protection

### Surface durability - Wear & Heat

#### Spills of: Water, Solvents, Acids & Alkalis

## Sanitation

### Barrier to contamination, dirt, grime etc.

## Appearance (Subjective)

### Type of wood and final surface condition

### Finish used and finishing schedule

# SOLVENTS

## Alcohol - Solvent for Shellac

### Denatured alcohol (Toxic Ethanol)

### Ethanol (grain alcohol) Liquor Taxes$$$

### Methanol (wood alcohol) toxic

### Flammable

## Lacquer Thinner - Solvent for Lacquer

### Mix of

#### Solvent - Ketones and Esters

#### Weak solvent - Alcohols

#### Thinner - Hydrocarbons (Toluene & Xylene)

#### % Content vary by brands

### Volatile Organic Compound Regulations

#### Toxic, Air Polluting and Flammable

## For Shellac & Lacquer remember

### “LIKE DISSOLVES LIKE”

## SOLVENTS Cont.

## Glycol Ether - Solvent for Water-base

### Complex combination of solvents

### Bridging Solvent - Makes solvent soluble 	substances compatible with water results in:

#### Water-Based finishes

#### NGR (non grain raising) dyes

## Mineral Spirits - Solvent for Waxes

### Thinner for Varnishes

# EVAPORATIVE FILMS
SHELLAC & LACQUER

## SHELLAC - Moderately Durable Film

### Natural resin secreted by Lac bug

### Solvent is Alcohol

### Used for high end antique repair/restoration

### Excellent resistance to water-vapor exchange

### More durable than blends of Oil &Varnish

### Versatile Application - spray, brush, pad

#### Very Quick to cure

#### Brushing -  need to keep wet edge

### Excellent Sealer or Barrier coat

#### Between wood/stains/topcoat finishes

#### Wash coat partial seal to reduce splotching

### Flakes (Blond - Amber - Garnet)

#### Waxed or De-waxed

#### 1 year shelf life after mixing

### Color with alcohol based dyes

### 1 LB. CUT (1 lb. flakes & 1 Gal. Alcohol

###### (1 oz. flakes & 8 oz. Alcohol)

### Pre-mixed typically 3 lb. cut, there is a shelf life

## LACQUER - More Durable Film

#### Complex material

##### Nitrocellulose (from cotton or wood + resin)

#### Solvent is Lacquer thinner

### VOC restrictions and flammable

## Evaporative Film advantages

### Solvents  “LIKE DISSOLVES LIKE”

### Build with subsequent applications

### Easy Finish Rubout and Repair

### Caution Dye dissolved in a solvent is re-dissolved by that solvent

# REACTIVE FINISHES
VARNISHES & OILS
Film & Penetrating

## Reactive Finishes

### Chemically change as they cure

### 1. Cross linking or Polymerization with oxygen

### Driers accelerate cure time

### 2. Reaction with an added catalyst

### Ex. conversion varnish, epoxy, cat. Lacq.

## Varnish Very Durable Film

### Resin + Oil and Heat

#### Resins - Alkyd, Phenolic & Polyurethane

### Brush on - Heavy build - Slow Cure

## Wiping Varnish

### Varnish thinned with mineral spirits

### Easy Application wipe on & wipe off

### Shorter cure time

### Thinner film need to build

### Examples:

#### Waterlox, Behlen Salad bowl

#### Miniwax wipe-on poly

### Might be labeled as Oils (misleading)

## Varnish and Oil Blend (Film)

### Softer finish

### Longer cure time

### Examples:

#### Ex. Watco, Behlen’s Danish or Teak oil

#### Deft Danish, Miniwax’s Antique or Tung oil

### Often labeled as Oils (misleading)

## Polymerized Oils(Film)

### Typically Tung Oil

### Heated in Oxy. free environment

### Increased hardness & reduced cure time

### Expensive

## Straight Oils (Penetrating)

### Curing Oils-  Tung and Boiled Linseed oil contains driers

### Semi Curing oils - Walnut, soybean, safflower

# WATER- BASED
FINISHES

## Promoted by Clean Air Act of 1990

## Advantages

### Less odor & less VOC content than Lacquer

### Faster drying than oil & oil based Varnishes

### More durable than Shellac

## Coalescing Cure

## Solvent based (much less solvent)

### Cured droplets dispersed in Water

#### Acrylic or Polyurethane resins

### Two solvents - Water and Glycol Ether

#### Water evaporates first after which the droplets (come together) coalesce and as the glycol ether evaporates a continuous film is formed.

## Conclusions of recent Product test

#### by Taunton’s Fine Woodworking

### Contrasts test results between 1995 and 2006

### 13 Brands broadly tested in the following three categories application, durability & appearance.

### Results demonstrated most brands had significant improvements and the best were as good as solvent-based finishes.

### Raising of grain not an issue for some.

# Waxes

## Paste Wax attributes:

### Ease of application

### Long lasting shine

### Can modify with colors

### Easy to renew or repair

### Wax does not stop water penetration; the water	does bead on the surface but also penetrates.

## Higher melting temps. >> Harder

### Carnauba - 180 F hard to buff

### Beeswax - 150 F

### Paraffin - 130 F soft will smudge

## WAXES Cont.

## Commercial waxes are a blend of these with a melting point of about 150 F

### Evaporation times vary depending on solvent Solvents- Mineral Spirits, Turpentine & Citrus

## Wax Polish on a table top protects the	FINISH from scuffs & scrapes

### Wax used alone provides the least protection if a durable usable surface is desired.

## Do not use clear wax on dark woods, clear wax will lodge in open pores.

## Wax is used as a finish for turnings and carvings that won’t be handled much.

# COLORING WOOD

## Methods of coloring

### Color wood directly

### Apply between topcoats (glazing)

### Add color to topcoat (toning)

## Coloring Products are often a combination of pigment stains and dyes.

## PIGMENTED STAINS

### Pigment is Opaque

### Enhances porous grain woods (oak, ash)

#### After wiping excess off pigment remains in open pores

#### Insufficient wiping leaves muddy appearance (painting)

## DYES (Liquid & Powder)

### Transparent - Enhances wood’s figure

### Powder Solvents: Water, Alcohol and Oil (M.S. or lacquer thinner)

### Dye molecules penetrate and saturate wood fibers

#### Hence less contrast between different sized pores.

###### (Minimize early wood and late wood contrast)

## Wood’s Grain is a factor when coloring

### You can match the color but not the woods grain

### Tight grained hardwoods: Maple, Birch & Cherry

### Medium grained hardwoods: Walnut & Mahogany

### Course grained hardwoods: Oak & Ash

### Soft woods: Pine & Fir

## COLORING Cont.

## Lightfastness - measure of color’s fading

### Manufactures provide a scale to rate

### Usually dyes (water) fade faster than pigments

### NGR (non grain raising) dyes are more lightfast

### Some topcoats have UV inhibitors that help

# FOOD SAFE?

## FLEXNER’S Summary:

### American Woodturner Spring 2008

## FDA lists ingredients and Manufactures need to formulate so they will cure.

### Non Lead driers need to be fully cured

## Finishes Advertised as food safe

### Oils: for example Walnut

### Some are Varnish based with driers added

## Flexner’s test - SMELL IT

### Any trace of solvent it is not cured

# PRODUCT TESTS

## FINE WOODWORKING PRODUCT TESTS

### Wipe on Finish Tests - Aug. 2005 #178

#### MINIWAX Wipe On Poly finish

#### WATERLOX Original High Gloss finish

### Waterborne Finishes -Dec. 2006 #187

#### GENERAL FINISHES High Performance

#### HYDROCOE RESISTHANE PLUS

### Wood Glues - Aug. 2007 #192

#### PVA Type I waterproof (Titebond)

#### PVA ( Elmers Carpenter’s}

# INFORMATION

## Material Safety Data Sheet (MSDS)

### Provides product’s chemical makeup, %solids etc.

## Color Wheel - A guide to mixing colors

### Can purchase @ Staples

## The Finishers Colorwheel

### By Color Concepts INC.

## Film Build (cured)

### (%Solid content) x (Wet Film Thickness)

#### 1lb cut shellac = 14% solids

#### 3lb cut shellacs = 31% solids

### Desired wet film (spray or brush) = 3 mil = .003 in.

# Sources of Information

## Understanding Wood Finishing

### By Bob Flexner

## Finishing

### By Jeff Jewitt

## Issues of Fine Woodworking Magazine

## Journal of the American Association of 	               		Woodturners

###### T. Sullivan 2/09